## Slide 1: The Promising Use of Volcanic Silica Rocks as an Environmental Source for Diagnostic X-ray Shielding Applications
Dr. Mohammed Damoom
Nuclear Engineering Department
King Abdulaziz University

## Slide 2: Contents
Introduction
Motivation and Objectives
Methodology
Results and Discussion
Conclusion

## Slide 3: Introduction

## Slide 4: Why Ionizing Radiation Dangerous?
Source: Clinical proceedings - Children's Hospital of the District of Columbia 1961.

## Slide 5: Radiation Hazard Scale
Source: Centers for Disease Control and Prevention

## Slide 6: Reducing Radiation Hazard
Source: US EPA

## Slide 7: Shielding Materials
Source: MarShield

## Slide 8: Concrete and CO2 Emission
Source: psci.princeton.edu

## Slide 9: Motivation and Objectives

## Slide 10: Motivation
Replacing concrete with natural building materials will help reduce CO2 emissions.
Berkeley Castle, UK.
The castle's origins date back to the 11th century
Stones last for a very long time (1000s years) compared to concrete (50 to 100 years).

## Slide 11: Objectives
Investigating the shielding properties of VSRs against diagnostic x-rays.
Comparing the radiation shielding properties of VSRs to that of concrete.

## Slide 12: Methodology

## Slide 13: Material Composition
Using the EDX analysis, the elemental compositions of volcanic silica and ordinary concrete were determined.

## Slide 14: Setup and Procedures

## Slide 15: Results and Discussion

## Slide 16: Mass Attenuation Coefficients
The figure shows that the mass attenuation coefficient values of VSR are almost as same as that of concrete.

## Slide 17: Mass Absorption Coefficients
The figure shows that the mass absorption coefficient values of VSR are almost as same as that of concrete.

## Slide 18: Half-Value Layer
The figure shows that the HVLs values of VSR and concrete are almost the same in low energies .
They are a little bit different in large energies.

## Slide 19: Mean Free Path
The figure shows that the MFP values of VSR and concrete are almost the same in low energies .
They are a little bit different in large energies.

## Slide 20: Variance
VSR = Volcanic Silica Rocks
Conc = Concrete
Variance for both materials are close to each other

## Slide 21: Conclusion

## Slide 22: Conclusion
The VSR can be used instead of concrete to shield against diagnostic x-rays.
The thickness better to be 15 cm or more