Development of Fusion technologies at ENEA

Brasimone Research Centre

Daniele Martelli, Alessandro Del Nevo, Massimo Angiolini, Agostini Pietro, Mariano Tarantino, Marco Utili, Marica Eboli, Pietro Arena, Alessandro Venturini, Francesca Papa, Ciro Alberghi, Serena. Bassini, Sebastiano Cataldo, Paolo Favuzza, Amelia Tincani, Davide Bernardi, Francesco S. Nitti, Chiara Ciantelli, Carlo Cristalli, Marco Lamberti.

# ENEA, Fusion and Technology for Nuclear Safety and Security Department, Italy

Località Brasimone, 40032 Camugnano (Bologna)

*Corresponding author:daniele.martelli@enea.it

Abstract – In the European fusion project, the ENEA Department of Fusion and for Nuclear Safety technology coordinates the Italian fusion program supported by third parties (universities, Italian research institutes and industries). In particular, the ENEA Experimental Engineering Division with headquarter in the Brasimone RC, designs, develops and characterizes technologies and materials related to the Water-Cooled Lithium Lead (WCLL) Breeding Blanket (BB) and the connected ancillary systems. The WCLL is a BB concept featured by pressurized water as the coolant and Lithium-Lead Eutectic (LLE) enriched at 90 % in 6Li as the breeder, neutron multiplier and tritium carrier.

ENEA research team is involved in the design of a multipurpose experimental infrastructure conceived to investigate and qualify water and LLE technologies for the DEMO BB and balance of plant systems. The proper design of the WCLL-BB is related to the capability of tritium extraction in the BB to be rerouted as fuel in the plasma chamber to achieve the self-sustainability goal. To successfully meet this task, experimental activities are carried out to characterize different T-extraction technologies (e.g. Gas-Liquid Contactor-GLC and Permeator Against Vacuum-PAV systems). In these tests, hydrogen and deuterium are used in the experiments as “cold surrogate” of T for safety issue. Special attention is dedicated to the development, optimization and characterization of structural and functional materials having low activation, chemical compatibility, enough ductility, and creep resistance at higher temperatures and dpas. Moreover, the protective coatings represent an important R&D area to enhance materials functionality.

Other relevant research tasks are dedicated to the development of reliable instruments to control key operative parameters, such as flow rate (development of a novel thermal flow meter), Q (hydrogen isotopes) concentration in PbLi (development of Hydrogen Permeation Sensor) and to the characterization of physical properties such as the tritium solubility and diffusivity in PbLi.

Keywords: WCLL, TBM, ENEA, DEMO, FUSION, Breeding Blanket

I. Introduction

The Experimental Engineering division (FSN-ING) of the ENEA department of Fusion and Nuclear Safety Technology coordinates the Italian fusion program for the development experimental and numerical setup.

The research activities are mainly devoted to: i) design of the Water Cooled Lithium-Lead Breeding Blanket (WCLL-BB) and PbLi/H2 interaction; ii) development of tritium extraction technologies from lead-lithium (PbLi); iii) experimental testing of the European DEMO Divertor mock-ups; iv) screening on corrosion and on the mechanical properties of the Reduced Activation Ferritic Martensitic (RAFM) alloys; iv) development of alumina-based as tritium barrier and anti-corrosion coatings and v) erosion/corrosion investigation in pure lithium flowing conditions

II. WCLL Design and PbLi/H2 interaction

In the framework of the EUROfusion activities on the Breeding Blanket, the ENEA Brasimone R.C. is responsible of the design of WCLL-BB concept. This means that FSN-ING division coordinates the work carried out by its own researchers, its Affiliated Entities (universities and industrial partners) and other foreign research institutions involved in the WCLL BB design.

The WCLL BB is one of the two concepts currently candidate to become the driver blanket of the EU-DEMO fusion reactor [1]-[3]. This BB concept envisages the adoption of water at PWR conditions (15.5 MPa of pressure and temperatures between 295°C and 328°C) as coolant, whereas the eutectic PbLi alloy as neutron multiplier, tritium breeding and carrier medium. The tritium produced by nuclear reactions occurring between lithium and neutrons is recovered by means of a dedicated system, the Tritium Extraction and Removal system (TER) [4]. This system is also in charge of circulating the liquid PbLi towards and from the BB. The structural material of both systems is the RAFM stainless steel EUROFER.

Both PbLi and cooling water are routed to each segment by means of feeding pipes entering the Vacuum Vessel from the lower (PbLi inlet) and upper ports (PbLi outlet, water inlet and outlet). Two independent cooling systems are foreseen for the BB, one devoted to cool the First Wall (FW) and another aimed at removing the thermal power deposited within the Breeding Zone (BZ).

The EU-DEMO BB is articulated in 16 toroidal sectors, each of one composed of three outboard and two inboard segments [1]. With reference to the WCLL BB, the internal structure of each sector envisages the reproduction along the poloidal direction of an elementary structure called elementary cell or “slice” [2][3]. Each slice (Fig. 1) consists of a box envisaging a C-shaped FW cooled by means of square channels and coated with a 2mm tungsten armour, radial-toroidal stiffening plates to separate the different slices and stiffen the segment, a manifold system for the distribution and recollection of PbLi and water, as well as a 100 mm thick Back-Supporting Structure (BSS) to sustain dead and Electro-Magnetic (EM). The BZ is cooled by means of bundles of Double Walled Tubes (DWTs).

Thanks to these design choices it is possible to ensure at the same time:

- the integration of both PbLi and water manifold in the blanket segment, enhancing the compactness in radial direction;

- a good structural behaviour thanks to the symmetrical thermal field and the segment robustness against EM loads arising from plasma instabilities;

- the optimization of the nuclear performances, such as the maximization of the Tritium Breeding Ratio (TBR) and shielding performances, as a consequence of the continuity of the structures and the elimination of particle streaming;

- the facilitation of the PbLi fill and drain procedures, as well as the removal of helium bubbles formed in the BZ and not dissolved in the PbLi.

Fig. 1: View of a WCLL BB segment and an equatorial slice.

Nevertheless, some open points need still to be addressed prior the Conceptual Design is reached. One of the most important and widely experimentally investigated at ENEA Brasimone R.C. is the interaction between PbLi and water, occurring as a consequence of an in-box Loss Of Coolant Accident (LOCA) in the BZ of the WCLL BB. Indeed, during a postulated in-box LOCA event, one of the high-pressure water-cooling pipes inside the breeding zone is supposed to break, even though the use of DWT. The interaction PbLi/H2 causes a violent energy release, both due to the thermodynamic and the chemical interactions between the fluids. Furthermore, the exothermic reaction contributes to increase the pressure and temperature and poses a safety risk due to the production of hydrogen. The evaluation of the consequences is of primary importance for the WCLL BB design, to assure the mechanical resistance of the component itself, or in the worst case, to avoid jeopardizing the entire system, as well as the prediction of the system behaviour under accidental conditions. Therefore, in recent years, R&D efforts have been focused on the strategy to face up the WCLL in-box LOCA scenario and for set-up qualified system codes for the deterministic safety analysis (DSA) [5]. In this framework, LIFUS5/Mod3 separate effect test facility was conceived to generate experimental database for phenomena investigation and code validation. Two experimental campaigns have been executed and provided reliable and repeatable data to validate the chemical reaction model implemented in SIMMER code, to enlarge experimental database, to support the new STH/2D coupling calculation tool [6]. The generated data have been used for code validation following a standard methodology, based on a three-steps approach and evaluating the accuracy of the numerical predictions from qualitative and quantitatively point of view, comparing experimental and calculated time trends.

As future step in supporting the design and validation activities of both the DEMO WCLL BB and the ITER-WCLL (TBM), the Water-thermal-HYDRAulical (W-HYDRA) experimental platform is currently under the design phase at the ENEA Brasimone R.C. To this purpose, W-HYDRA platform will have a strategic role since it will allow to test technologies and components at relevant BB and TBM conditions. The experimental platform envisages three main facilities sharing some areas and components: i) Water Loop (WL), ii) STEAM and iii) LIthium FUSion 5 Mod 4 (LIFUS5/Mod4).

The WL is a medium scale facility whose main goals are the testing of the full-scale WCLL TBM, the development and testing of medium-scale mock-ups for the WCLL BB, as well as offering the possibility to test the thermal-hydraulic and thermo-mechanic performances of components subjected to high heat fluxes (e.g. plasma facing components).

The WL will represent an Integral Test Facility for the WCLL-TBM and its related Water Cooling System (WCS). Indeed, the WL design reproduces the WCS features in terms of functions, layout and components, to performing thermo-hydraulic and structural tests on a WCLL-TBM mock-up. Moreover, since WL will be equipped with the same control logics and safety components foreseen for the ITER WCS, it will be able to perform safety related tests, such as LOCA and Loss Of Flow Accident (LOFA) scenarios occurring to the ITER WCS circuit. This will allow the achievement of multiple goals: the verification and validation of the numerical model set-up during the pre-conceptual and conceptual design phases, the possibility of performing a training for ITER operators, the testing of sensors and other instrumentation, etc.

On the other hand, prototypical BB mock-ups (FW, Breeding Zone, manifolds, etc.) will be tested under relevant thermo-hydraulic and thermo-mechanical conditions. This will be possible thanks to a high-flow rate branch of the loop (for the BB manifold) and the availability of a 25m³ vacuum chamber equipped with an 800kW Electron Beam gun.

As far as STEAM is concerned, it is an experimental facility capable to investigate one of the most critical components of the DEMO WCLL Balance of Plant (BoP), the Steam Generator (SG) of the BB Primary Heat Transfer System (PHTS).

The objective of the water-water SG test campaign is to demonstrate the capability of this component to perform as intended during the different power phases of the DEMO period that, according to the present concept design assumption, consists of a 2-hour pulse at full power followed by 10 min of dwell at decay power. This scenario identifies three operational phases of the SG:

- a low power phase representing the DEMO dwell period. The main investigation will focus on the thermal-hydraulic stability of the component operation at low power and its performance, as well as on the effectiveness of the regulation strategy adopted. This phase will be crucial for the demonstration of the BoP reference concept since the SG power duty is very far from the minimum values suggested by the standard practice;

- the full power phase representing the DEMO full power conditions. Even though it is expected that the SG does not experience any issues during this phase, it remains mandatory to demonstrate the adequacy of the adopted design and the reliability of the numerical simulations. Indeed, available current System Thermal-Hydraulic (SYS-TH) codes are not qualified for this type of Steam Generator;

- the transient phase, reproducing the transition from pulse to dwell operation. The main focus will be on the performance of the component and the suitability of the adopted control strategy. It will include also tests aiming at identifying the domain enveloping the operational TH parameters for a safe, stable and efficient performance of the SG. This phase will complete the demonstration of the functional feasibility of the SG of the WCLL BB BoP architecture with direct coupling in the DEMO pulsating scenario.

LIFUS5/Mod4 is a PbLi loop based on that foreseen for the ITER WCLL Test Blanket System (TBS). This facility will have an interface with the WL to perform experimental tests on the PbLi/H2 interaction aimed at the validation of the numerical models and tools currently adopted for its modelling.

Two different experimental phases are foreseen, in the first one, the main objective will be the test of the response of the WCLL-TBS in case of in-box LOCA scenario and the measurement of relevant thermo-dynamical parameters throughout the facility. To achieve this goal, it is necessary that the facility is as much representative as possible of the operative conditions and hydraulic behaviour of the real system (i.e. the WCLL TBS PbLi loop). The only planned difference between the LIFUS5/Mod4 and the TBS PbLi loop will be represented by the absence of the circulation pump in the LIFUS5/Mod4 loop. The expected outcomes of these experimental activities are the acquisition of relevant and significant data in support of code validation, as well as the design improvement of the WCLL-TBS components and layout.

In the second phase, the test of all the systems and functions implemented in the TBS during normal operation scenarios is planned. To this purpose, the facility will be upgraded with the PbLi circulation pump. The expected outcomes are the optimization of control strategies, individuation of criticalities in system design or operation, optimization of subsystems design, measurement of system performance. To achieve these goals, WL and LIFUS5/Mod4 facilities will be coupled, representing the first example of separate test effect facility for the investigation of the water/PbLi interaction in a WCLL representative geometry. Experimental test carried out in LIFUS5/Mod4 will allow to extend the validation of numerical model set-up with different codes (Simmer III and IV, RELAP5) to WCLL relevant geometries.

III. Tritium Extraction from PbLi

For the self-sufficiency of the fusion reactor and for the minimization of tritium release towards the external environment a tritium extraction and removal system from PbLi is a critical issue. Different types of tritium extractors from PbLi are under characterization at ENEA Brasimone: i) Gas-Liquid Contactors (GLCs) in the packed column configuration and ii) Permeation Against Vacuum (PAV). These technologies are experimentally investigated with the support of the experimental facility TRItium Extraction II (TRIEX-II, Fig. 2) [7]. A mock-up of GLC, 1:1 ITER TBM scale, was characterized in TRIEX-II at 400 and 450 °C in the liquid metal flow between 0.2 and 1.2 kg/s. The facility can supply a maximum LLE flow to the test section (TS) of 6 kg/s in the temperature range between 300 and 530 °C. The PbLi is pumped in the facility with a permanent magnet pump and is sent to the TS.

Fig. 2:  TRIEX-II facility (PAV configuration)

The Q is solubilized inside the PbLi with a GLC saturator, where the Q2 is injected inside the saturator through a gas injector system, in a mixture with helium. The saturator allows the alloy to reach the desired hydrogen or deuterium concentration, which simulates the WCLL-TBM/BB outlet composition of PbLi.

The PAV mock-up (Fig. 3) is based the phenomenon of tritium permeation through a membrane (such as α-iron, vanadium or niobium) in contact with PbLi towards a secondary side where vacuum is pumped. Vacuum is needed to keep a partial pressure gradient between the two sides of the membrane, so that permeation can take place. The tested mock-up is composed by a cylindrical vessel with 16 niobium U-tubes, the membranes for hydrogen permeation, welded on a F22 plate. Vacuum (lower than 1 Pa) is pumped in the vessel while the PbLi flows in the niobium pipes.

ENEA, in collaboration with Politecnico di Torino,

developed sensors dedicated to the measurement of hydrogen isotopes partial pressure [8]. These sensors (Fig. 3) are called hydrogen permeation sensors (HPS) as they are based on the physical principle of permeation of hydrogen isotopes through a membrane (same concept of the PAV system). Hydrogen permeation sensors are composed by a permeable helical-shaped pipe (Figure 3), closed at one end and immersed in the PbLi, a vacuum pressure transducer, a vacuum valve and a vacuum station (membrane pump plus turbomolecular pump). The efficiency of the GLCor PAV component is evaluated from the concentration measurement before and after the components.

Fig. 3: PAV Mock-Up (Niobium tubes),left, HPS, right

IV. DEMO Divertor Mock-Up

Within the EUROfusion Programme ENEA Brasimone R.C. has been involved in the experimental testing of the European DEMO Divertor [9] mock-ups.

A full-scale mock-up of the DEMO Divertor Outer Vertical Target (OVT) has been installed and tested in the CEF1 experimental hall [10] (Fig. 4).

Fig. 4: OVT Mock-Up

The experimental campaign had two main objectives: i) verify the hydraulic design and its capability to ensure a uniform and proper cooling for the Plasma Facing Units (PFU) with an acceptable pressure drop across the inlet and outlet sections of the mock-up, and ii) experimentally validate the computational fluid-dynamic (CFD) model developed by the University of Palermo.

Both objectives have been successfully achieved through the experimental tests carried out in stationary conditions. In fact, the overall pressure loss at the reference mass flow rate of 54.95 kg/s has been close to the design value calculated for the DEMO OVT (about 7.4 bar). The distribution of the water mass flow rate among the plasma facing channels has been found to be sufficiently uniform, being the maximum variation within the ± 10% of the average value. Finally, the CFD model has been preliminary validated. Indeed, the theoretical–numerical results have exhibited an overall good agreement with experimental data, being the maximum error on pressure drop estimation equal to − 7.22% and for the comparison of the coolant flow distributions among PFU channels the maximum error predicted equal to 9.36%, while the average error has a maximum of 3.11%.

For details on the OVT mock-up, instrumentations, test campaign results and validation of the computational fluid-dynamic (CFD) model see reference [10].

V Structural materials and corrosion

V.A. Structural Materials and corrosion

In the frame of the EUROFUSION Work Package Material (WPMAT), ENEA Brasimone R.C. has been involved in the screening on the mechanical properties of the RAFM (Reduced Activation Ferritic Martensitic) alloys proposed as optional to Eurofer as structural materials for the DEMO Breeding Blanket.

For low temperature applications (DEMO Water Cooled Breeding Blanket) the target is the development of strategies aimed at the grain size refinement, due to the positive effects of grain size reduction on toughness [11]-[12]. Moreover, a nano-structured alloy should exhibit better resistance to the low temperature irradiation hardening, due to the increase in recombination probability of point defects on grain boundaries and should be more tolerant respect to the Helium embrittlement phenomena. With this aim, we studied the effects of thermo-mechanical treatments (multiple annealing and recrystallization treatments) and chemical composition variations (acting on key elements, like Tungsten, Tantalium, Niobium and Vanadium) to obtain nano-structured alloys and the effects of these treatments on toughness (KLST tests) and tensile properties; the recrystallization thermo-mechanical treatment taken into account consists of a cold-working followed by low temperature tempering, carried out after the usual normalization and tempering treatment. Unquestionable benefits have been detected by means of this treatment on grain refinement. On the other hand, concerning high temperature applications (DEMO Dual Coolant Breeding Blanket), the newly produced alloys have been characterized in different metallurgical conditions, in terms of tensile, creep, impact, LCF (Low Cycle Fatigue) and CF (Creep-Fatigue) tests. A series of LCF tests has then been carried out at 650°C on the 3126 alloy in two metallurgical conditions (ausformed at 650°C or without ausforming) varying the total strain amplitude (from 1 to 0.3 %). The threshold of 10000 cycles has been achieved for a total strain amplitude lower than 0.4%. At 0.3 % strain range, three HT (hold time) durations have been selected (40s, 80s and 200s) for the tests in CF condition. The CF tests substantially confirm the ASME diagram used to evaluate the Creep Fatigue Interaction on martensitic alloys.

V.B. Corrosion

Corrosion in molten PbLi eutectic is a major issue in the design of the BB due to the high chemical aggressiveness of the liquid metal. Steels suffer of severe solution-corrosion and in the case of the RAFM steel EUROFER - the candidate material for DEMO WCLL breeding blanket – the metal loss can reach rate of 400 µm/year at 550°C in flowing conditions [13].

To support the design of the WCLL blanket for DEMO and the development of purification systems for the PbLi loop, ENEA Brasimone is involved in the study of the corrosion of EUROFER in PbLi eutectic both in fresh and “contaminated” PbLi. Exposure tests of EUROFER in fresh PbLi were performed in stagnant conditions at 550°C up to 8000h in the RACHEL laboratory, described in [14]. Stagnant tests were performed since relevant for the low PbLi flow velocity expected in WCLL blanket (few mm/s).

The corrosion rate in fresh PbLi shows typical power dependency on time and the corrosion was 18 µm/yr [14] as shown in Fig. 5.

Fig. 5: Comparison of the corrosion rate of EUROFER in fresh LiPb and with addition of Fe impurities in stagnant LiPb at 550°C

Post-test examination on samples shows almost-uniform corrosion of EUROFER with formation of porosity, and slight depletion of Cr (Cromium) and W (Tungsten) enrichment at the interface due to the different solubility of these elements [14]. A surface picture of 8000h exposed sample is in Fig. 6: it is possible to observe the morphology of the corroded portion (porous) in comparison with a protected area from LiPb exposure (smooth). Considering as reference the corrosion rate in “fresh” LiPb, the exposure tests with contaminated LiPb were performed at the same temperature 550°C up to 4000h with different dissolved Fe concentrations obtained by solution of Fe powders in the melt and equilibration. The results indicated that corrosion rate of EUROFER is lower in Fe-contaminated tests compared to that obtained with fresh LiPb (Fig. 5) but the morphology of corrosion has the same peculiarities.

Fig. 6: Surface picture of EUROFER exposed to 8000h showing the morphology of the corroded and protected areas.

VI. Coating development

As described in the previous chapter, RAFM steel are affected by corrosion when exposed to PbLi. Moreover, tritium generated in the BB tends to permeate through EUROFER walls in the cooling water circuit following the concentration gradient. To cope against those issues, research is going on at ENEA Brasimone R.C. on alumina barrier coatings since aluminium oxide has been considered as a reference material for those functional coatings considering its chemical stability in the PbLi environment and its excellent tritium permeability barrier action [15]. Coatings are being realized by different deposition techniques such as Pulsed Laser Deposition (PLD)[16] and Atomic Layer Deposition (ALD)[17]. Among these deposition techniques, the PLD is currently the most explored, and Al2O3 coatings deposited by this method demonstrated PbLi corrosion resistance and anti-diffusion performance against several gaseous species. [18].

EUROFER samples covered with 3 and 5 μm thick PLD coatings have been tested in static PbLi at 550°C at the RACHEL laboratory while for the fluent PbLi test, EUROFER specimens with 3 µm PLD coating have been introduced and exposed in the IELLLO (Integrated European Lead Lithium LOop) facility at 500°C and with a mass flow rate corresponding to an average velocity of 0.5 m/s. Observation performed by Scanning Electron Microscopy (SEM) revealed a good adhesion at the coating/steel interface and no thickness variation of the alumina coating after the exposures of 7000 h for the static PbLi test and 4000 h for the fluent PbLi one. Moreover, no traces of corrosion have been detected underneath the coating inside the EUROFER substrate, as confirmed through SEM and Energy Dispersive X-Ray spectroscopy (EDX) investigation, indicating that the structural steel resulted protected against the PbLi corrosive action. Nevertheless, investigation executed on the coating surface by different analysis techniques (XRD, SIMS, XPS, Atom Probe Tomography etc.) highlighted a chemical interaction between the alumina and the lithium in the PbLi in the first micrometers of the coating, indicating the formation of some amount of Li-Al mixed compounds. The presence of those hybrid species inside the coating maybe detrimental as this can diminish corrosion resistance and tritium anti-permeation performance. For those reasons, the extension and nature of the alumina-lithium interaction must be better understood and is currently under investigation.

VII Erosion/corrosion in pure lithium flowing conditions

ENEA Brasimone research activities are also focused on the characterization of pure liquid Lithium (Li) behaviour for its suitable employment in fusion applications. In this regard, it must be highlighted that this alkali metal will serve as the neutron flux generator of the IFMIF-DONES facility [19] (WPENS).

For about 20 years, ENEA Brasimone has been hence involved in the study of the erosion-corrosion action exerted by flowing liquid Lithium on plant structural materials, like austenitic and RAFM steels. A lab scale plant called Lifus3 was at first designed, realized and employed for this purpose; later, since the second decade of this century, a new plant, Lifus6, replaced the previous one, introducing significant optimizations and additional features: this plant is nowadays still under operation.

Lifus6, whose 3D design is shown in Figure 1, is essentially constituted of two different loops, mounted on a steel frame:

- the main loop (isotherm), where Li flows at the maximum rate of 30 l/min and the max temperature of 350°C, and which houses the TS for the insertion of the specimens under investigation; according to the design of the TS, Lithium can reach here the maximum speed of 15m/s.

- the secondary loop, where Li flows at ~ 0.3 L/min and which houses i) the Cold Trap (200-210°C, for purification of Lithium from non-metallic impurities like Carbon, Oxygen and Hydrogen); ii) the Resistivity Meter, able to online monitor the total concentration of the impurities dissolved in the flowing Li; iii) a Li sampler (~ 25 mL) to quantify its Nitrogen (N) content.

The plant is additionally equipped with a Hot Trap where all the Li inventory can be statically kept at 550-600°C for long time, to be purified from N.

Fig. 7:LIFUS6

In a first Lifus 6 experimental campaign, specimens made of Eurofer 97 and F82H (RAFM steels) underwent 3 different erosion-corrosion tests for 4000 h, at 330°C, N concentration in Li < 30 wppm, Li velocity of 15 m/s. Obtained results indicated, for both the materials: i) a corrosion rate < 0.2 m/y; few and isolated corrosion phenomena on the exposed surface; a small depletion of Cr and W (-1.5 wt% max) in the alloy composition in the first surface layer [20]. In a second experimental campaign, Eurofer 97 and AISI 316L specimens were tested with the same conditions as before apart from the Ni concentration (increased to 320 wppm), resulting in a corrosion rate of ~ 1.3 m/y for the RAFM steel, and ~ 10.7 m/y for the austenitic one, in view of the presence of the high soluble N in the latter one. The outcome of the tests also confirmed that the presence of N impurities in Li greatly enhances the corrosion exerted by the alkali metal, due to the formation of a ternary Li-N-Cr compound [21].

Due to the negative effect produced by high concentrations of dissolved N, the control and removal of this element from Li becomes hence mandatory; to find out the best solid material (getter) able to quantitatively accomplish this purification procedure, an additional facility, named ANGEL, has been recently designed and constructed in ENEA Brasimone R.C., and it is currently under operation. In this facility, up to 4 different solid materials (generally transition metals or alloys) can be simultaneously tested as potential getters for N; each of them is put in contact with the same kind of liquid Li, characterized by the same N concentration (preliminary fixed as desired) and at the same temperature (up to 600°C), but each one in its own separate vessel. Each vessel is equipped with 4 lateral arms acting as samplers that can be filled by Li from the main body at different, defined time spans during the test (generally lasting about 20 days); after determining the N contented in the 4 Li samplers, it is hence possible to monitor the N removal by the getter with time, for each of the investigated getters.

Acknowledgments

This work has been carried out within the framework of the EUROfusion Consortium, funded by the European Union via the Euratom Research and Training Programme (Grant Agreement No 101052200 - EUROfusion). Views and opinions expressed are however those of the author(s) only and do not necessarily reflect those of the European Union or the European Commission. Neither the European Union nor the European Commission can be held responsible for them.

References

- L.V. Boccaccini et al., Status of Maturation of Critical Technologies and Systems Design: Breeding Blanket, Fusion Eng. Des 179 (2022) 113116;

- P. Arena et al., The DEMO Water-Cooled Lead-Lithium Breeding Blanket: Design Status at the End of the Pre-Conceptual Design Phase, Appl. Sci. 11 (2021) 11592;

- P. Arena et al., Design and Integration of the EU-DEMO Water-Cooled Lead Lithium Breeding Blanket, Energies, 2023, 16, 2069;

- A. Del Nevo, et al., Recent progress in developing a feasible and integrated conceptual design of the WCLL BB in EUROfusion project, Fusion Eng. Des., 146 (2019), pp. 1805-1809;

- M. Eboli, et al., PbLi/water reaction: experimental campaign and modelling advancements in WPBB EUROfusion Project, Invited oral 32nd Symposium on Fusion Technology (SOFT2022), 18-23 September 2022, Dubrovnik, Croatia;

- M. Eboli, et al., Experimental and Numerical Results of LIFUS5/Mod3 Series E Test on In-box LOCA Transient for WCLL-BB, Energies 2021, 14, 8527;

- A. Aiello et al., TRIEX facility: an experimental loop to test tritium extraction system from lead lithium, Fusion Eng. Des. 82 (2007) 2294–2302;

- L. Candido et al., ‘Development of advanced hydrogen permeation sensors to measure Q2 concentration in
lead-lithium eutectic alloy,’ Fusion Engineering and Design, vol. 124, pp. 735–739, 2017);

- J.H. You, et al., Divertor of the European DEMO: Engineering and technologies for power exhaust, Fusion Engineering and Design 175 (2022) 113010;

- Amelia Tincani et al., Hydraulic Characterization of the Full Scale Mock-Up of the DEMO Divertor Outer Vertical Target, Energies 2021, 14, 8086;

- E. Gaganidze, J. Aktaa, Assessment of neutron irradiation effects on RAFM steels, Fusion Eng. Des. 88 (2013) 118–128;

- Y. Dai, et al., Neutron/proton irradiation and He effects […], J. Nucl. Mater. 415 (2011) 306–310.

- J. Konys, et al., Compatibility behavior of EUROFER steel in flowing Pb–17Li, Journal of Nuclear Materials 386-388 (2009) 678-681.

- S. Bassini, et al., Long-term corrosion behavior of EUROFER RAFM steel in static liquid Pb-16Li at 550 °C, Fusion Engineering and Design 160 (2020) 111829.

- E. E. Rönnebro et al., Recent Advances and Prospects in Design of Hydrogen Permeation Barrier Materials for Energy Applications—A Review. Molecules 2022, 27, 6528.

- A. J. Haideret al., A comprehensive review on pulsed laser deposition technique to effective nanostructure production: trends and challenges; Opt Quant Electron 54, 488 (2022).

- P. O. Oviroh, et al., New development of atomic layer deposition: processes, methods and applications; Science and Technology of Advanced Materials 20, 2019, 465-496;

- M. Utili et al., Development of anti-permeation and corrosion barrier coatings for the WCLL breeding blanket of the European DEMO; Fusion Engineering and Design, 170, 2021, 112453.

- D. Bernardi et al., The IFMIF-DONES Project: Design Status and Main Achievements within the EUROfusion FP8 Work Programme, J. Fus. Energy 41:24 (2022).

- P.Favuzza et al., Erosion-corrosion resistance of Reduced Activation Ferritic-Martensitic steels exposed to ﬂowing liquid Lithium, Fus. Eng. Des. 136 (2018) 1417–1421;

- J.Knaster, P.Favuzza, Assessment of corrosion phenomena in liquid lithium at T < 873 K. A Li(d,n) neutron source as case study, Fus. Eng. Des. 118 (2017) 135–14;